PRODUCT SPECIFICATION

(    AEROFLEX Closed Cell Elastomeric Thermal Insulations

| PHYSICAL PROPERTIES ( | AEROFLEX | TEST METHOD |
| --- | --- | --- |
| Cell Structure | Closed Cell | - |
| Density Ibs/ft3(kg/m3) | 3-6 (48-96) ((( | ASTM D 1667 |
| Thermal Conductivity BTU.in/ft2 hr. (F (W/mk) | Mean Temp. | -4 (F (-20 (C) | 32 (F (0 (C) | 75 (F (24 (C) | 90 (F (32 (C) | 104 (F (40 (C) | ASTM C 518, C 177 JIS A 1412 DIN 52613 |
|  | K-value | 0.22 0.032 | 0.23 0.034 | 0.25 0.037 | 0.26 0.038 | 0.27 0.039 |  |
| Service temperature (((( | -70 (F to 257 (F -57 (C - + 125 (C | AEROFLEX becomes Hard at -57 (C, but Can be used even at -200(C |
| Water Vapor permeability (g/Pa.s.m) | 0.10 perm-in (1.44x10-10) | ASTM E96 |
| Moisture Resistance (µ value) | µ( 7000 | DIN 52615 |
| Water Absorption (% by weight) | ( 5 | ASTM D 1056 |
| Ozone Resistance | No crack | ASTM D 1171, D 1149 |
| Heat Stability (% shrinkage) 200 (F (93 (C) 7 days | 6 | ASTM C 534 |
| Flammability & smoke, Density | Class V O | UL – 94 |
|  | 25/50 | ASTM E 84 |
|  | Self – extinguishing | ASTM E 635 |
|  | Class 5.3 | EMPA (Switzerland) |
|  | Non-Flammable | JIS K 6911 |
|  | Pass | IMO ((((( |
| U.V. Weather Resistance | Excellent | - |
| Corrosion of copper, stainless | Non corrosive | DIN 1988 |
| Nitrosamine Contents(((((( | Not Detected | U.S. FDA |
| Sound reduction ((LAF) | 27 dB (20 mm) | DIN 52218 |
| Flexibility | Excellent | - |

Specifications Company ASTM C534

(Figures show the average values obtained by the world well-known testing institutes

(( Tested according to DIN, JISASTM and others.

(((Average density of insulation thickness ( 20mm is 2.5 – 5 Ibs/ft3 (40 – 80 kg/m3)

((((At temp. under -57 CAEROFLEX become hard, but it doesn’t affect thermal conductivity nor  water vapor permeability.

In the heating applications AEROFLEX can Stan + 125 (C   continuously, and the adhesive upto +100 (C

(((((IMO : International Martime Organization, IMO fire test procedures code part 5 and part 2  [IMO res. A.653[16]]

- Lioyd’s type approval certificate

- DNY’s type approval certificate

((((((It is reported that Nitrosamine is harmful to human health even during storage. No Nitrosamine compound was

detected in AEROFLEX

| Properties | Aeroflex-Standard | Test Method |
| --- | --- | --- |
| Mold Resistance | Meet Requirement (Rating 1) | UL 181 |
| Fungi Resistance | No Growth | ASTM C1338 |
| Bacteria Resistance | Meet Requirement (Anti-Bacteria) | ASTM E 2180 |
| Corrosion of Copper/Stainless Steel | Non Corrosive | DIN 1988 |
| Nitrosamine Contents | Not Detected | FDA CPG 7117.11 |
| RoHS | Not Detected | EN Restriction of the Use of Hazardous Substances Directive (RoHS) 2002/95/EC |
| Sound Reduction (AF) | 32 dB(20 mm) | DIN EN ISO10052, DIN 4109-11 |
| Flexibility | Excellent | ASTM C 534 |